Our request is as following:

Molecular formula CH2=CHCN

Molecular weight: 53.06

Boiling point: 77.3 °C

Melting point: 5±0.05 @ 760 mm Hg

Specific gravity: 0.8004g/ml @20°C

Vapor density: 1.83 g/mᶟ @ 25°C

Critical temp: 246 °C (Air=1.0)

Critical press: 34.9 atm

Ignition point: 481°C

Flashing point: 0 °C

Explosion limit: 3-17 vol% In air

Combustion heat: 420.8 Kcal/mol @ 25°C, liquid

Vaporizing heat: 7.8 Kcal/mol @ 77°C

Polyrnerizing heat: 17.3±5 Kcal/mol

Solubility: 7.3 wt% @ 20°C Water

Purity: 99.5( wt% (ASTM D-3962)

Color, APHA: 10( @25°C (ASTM D-1209)

Acetone: 100( ppm (ASTM D-3962)

Water%: 0.5(wt (ASTM E-1064)

Acetaldehydes: 20( ppm (ASTM D-2110)

Acetonitrile: 100(ppm (ASTM D-3962)

HCN: 5( ppm

Inhibitor (MEHQ):35( ppm

Specific Gravity 0.799-0.802 @25°C/15.5°C